## Slide 1: Clay Mineral Image Collection for Education in Geotechnical Engineering and the Earth Sciences
Acknowledgements:
Creation of this image collection was supported by the National Science Foundation under Grant No. 1301124 "Biologically-Inspired Silicification of Fine-Grained Soils." Any findings, conclusions, or recommendations expressed herein are those of the authors and do not necessarily reflect the views of NSF.
Thiel Kaolin Co. and WyoBen, Inc. supplied the Kaolinite and Bentonite minerals, respectively.
Gordon Stone and Joseph Dove
Via Department of Civil and Environmental Engineering
Nizhou Han and Patricia Dove
Department of Geosciences
Virginia Tech
December 2015

## Slide 2: Copyright and Use
The material in this document is licensed under Creative Commons CC BY-NC 4.0. You are free to copy and redistribute the images in any medium or format. However, you agree to:
-Cite this document when you use any of the information contained herein.
-Use this information for non-commercial, educational purposes only.
Interpretations
We do not provide interpretations of the images. See the "notes" pane in each slide for associated metadata.

## Slide 3: Materials and Experimental Methods
Materials
1. Kaolinite: B80 kaolinite from Thiel Kaolin Co. of Sandersville, Georgia. 97.5% finer than the No. 200 sieve, 68% finer than 2 microns; liquid limit = 76 and plastic limit = 33.
2. Bentonite: Naturalgel from Wyo-Ben, Inc. of Billings, Montana. 97% finer than No. 200 sieve, 60% finer than 2 microns; liquid limit = 570, plastic limit = 68.
3. Local Blacksburg, Virginia soil. 88% finer than the No. 200 sieve, 55% finer than 2 microns; liquid limit = 71, plastic limit = 23. Mixed mineralogy.
Methods
Clays were used as received. Samples of the Blacksburg soil were passed through a No. 200 sieve prior to preparation for imaging.
Fracture surfaces. Compacted at optimum moisture using standard Proctor effort, freeze dried, and fractured using a razor blade. Sputter coated with Iridium.
Shear Failure Surface. Compacted at optimum using standard Proctor effort, then brought to failure in unconfined compression. Sample collected from shear failure surface then freeze dried and sputter coated with Iridium.
Slurry deposited samples. Dispersed in water, deposited on pedestal using medicine dropper then air dried. Sputter coated with Iridium.
Images were acquired at several "regions" on each sample. Within each region, images were collected at progressively higher magnifications. The image footer provides magnifications (i.e., Mag=1k x) and a bar scale. All images were collected in tiff format with a LEO (Zeiss) 1550 Field Emission Scanning Electron Microscope (FESEM) in the Nano Characterization and Fabrication Laboratory of Virginia Tech's Institute for Critical Sciences and Technologies.

## Slide 4: Kaolinite Fracture Surface
Specimens compacted at optimum moisture, freeze dried, and fractured using a razor blade (tensile fracture). Images collected by Gordon Stone.
Images are included from two samples that are made at progressively higher magnifications. They feature a compacted fabric matrix with a layer of loosely attached particles oriented in the direction of tensile fracture. These images highlight the morphology of Kaolinte, which can be clearly observed at the higher magnifications.

## Slide 5
Notes: Sample 1, Region 4

## Slide 6
Notes: Magnified view near the center of the previous image, #104785

## Slide 7
Notes: Magnified view of the center of the previous image, #104783.

## Slide 8
Notes: Sample 1, Region 5

## Slide 9
Notes: Magnified view near the center of the previous image, #104786

## Slide 10
Notes: Magnified view near the center of the previous image, #10477. Clay particles are covering a larger particle.

## Slide 11
Notes: Sample 1, Region 6

## Slide 12
Notes: Magnified view near the center of the previous image, #104789

## Slide 13
Notes: Magnified view near the center of the previous image, #104790

## Slide 14
Notes: Sample 2, Region 5

## Slide 15
Notes: Magnified view near the center of the previous image, #104801

## Slide 16
Notes: Magnified view near the center of the previous image, #104803

## Slide 17: Kaolinite Shear Failure Surface
A sample was compacted at optimum moisture and brought to failure in an unconfined compression test. The specimen for imaging was collected from the resulting failure surface, then freeze dried, mounted, and sputter coated. View in the images is of the failure surface.
All images collected by Gordon Stone.

## Slide 18
Notes: Sample 1, Region 1. Approximate shear direction shown by arrow. Note striations in direction of shear and the orientation of particles.

## Slide 19
Notes: Magnified view near the center of the previous image, #100071.

## Slide 20
Notes: Magnified view near the center of the previous image, #100072. Clay particles are oriented parallel to shear plane.

## Slide 21
Notes: Sample 1, Region 4. Approximate shear direction shown by arrow.

## Slide 22
Notes: Magnified view near the center of the previous image, #100082

## Slide 23
Notes: Magnified view near the center of the previous image, #100082 and is the upward pan of image #100083

## Slide 24
Notes: Sample 1, Region 5. Steps along the failure surface in an area of high shear surface complexity.

## Slide 25
Notes: Sample 2, Region 2. Small "particle" at upper right is an artifact from the imaging process.

## Slide 26
Notes: Magnification of kink band

## Slide 27: Kaolinite and Bentonite Mixture
60% Bentonite and 40% Kaolinite by weight, hydrated and mixed together in a slurry then deposited on SEM sample holder. Images are of the mineral layer remaining after air drying.
Images for this series collected by Gordon Stone, Department of Civil and Environmental Engineering
and
Steve McCartney, Institute for Critical Sciences and Technologies at Virginia Tech

## Slide 28
Notes: Sample 1, Region 2.

## Slide 29
Notes: Magnified view near the center of the previous image, #10906.

## Slide 30
Notes: Magnified view near the center of the previous image, #10907. 100 nm = 0.1 micron

## Slide 31
Notes: Sample 1, Region 3

## Slide 32
Notes: Magnified view near the center of the previous image, #10910

## Slide 33: Bentonite
Bentonite hydrated in a slurry, deposited onto FESEM platen and air dried.
Images for this series collected by Gordon Stone, Department of Civil and Environmental Engineering
and
Steve McCartney, Institute for Critical Sciences and Technologies at Virginia Tech

## Slide 34
Notes: Sample 1, Region 1

## Slide 35
Notes: This image is the magnification of the right-center of the image #8657

## Slide 36
Notes: This image is the magnification of the right-center of the image #8658. Note that there are particles visible.

## Slide 37: Natural soil from Blacksburg, VA
Soil hydrated in a slurry then deposited and air dried on FESEM platen. Soil is of mixed mineralogy consisting of Kaolinite and Illite/Smectite.
Images for this series collected by Gordon Stone, Department of Civil and Environmental Engineering
and
Steve McCartney, Institute for Critical Sciences and Technologies at Virginia Tech

## Slide 38
Notes: Sample 1, Region 1

## Slide 39
Notes: Magnified view near the top right corner of the image #8649

## Slide 40
Notes: Magnified view near the center of the previous image, #8650

## Slide 41
Notes: Sample 1, Region 2

## Slide 42
Notes: This image is the magnification of the center of the image #8661

## Slide 43
Notes: This image is the magnification of the center of the image #8662. 100 nanometers = 0.1 micron